Research Aims

The general objective of this dissertation is to evaluate the biotechnological potential of fungal melanin as an innovative biomaterial to be used in biorremediation of heavy metals and semiconductivity environmental and industrial applications. The research will focus on the black fungi as model organisms because of their strong melanization and extremophilic nature.

To develop this research project, the following specific objectives have been proposed:

I.	To assess the ability of several black fungi isolated from extreme environment to tolerate and remove two very relevant contaminants: As(V) and Cr(VI) chemical species.

II.	To develop and optimize a protocol for fungal melanin extraction and purification for subsequent in-depth physicochemical and structural characterization. This characterization will focus on elucidating the structure-function relationship of melanin, particularly regarding its electroconductivity and heavy metal sorption capacity.

III.	To asses the biochemical and genetic expression changes that occur in Exophiala mesophila when exposed to As(V) and Cr(VI). Additionally, it will explore the effect of DHN-melanin exposure on cell inhibition.

IV.	To evaluate the role of fungal melanin`s semiconductive properties in mediatin interspecies electron transfer to stimule electogenic bacteria. To explore the potential application of this mechanism for mitigating CH4 emissions.

Discusión general

Melanin possesses a unique combination of desirable properties for practical applications. These include biocompatibility, photoprotection, metal chelation, toxin binding, and antimicrobial activity. However, both animal-derived and synthetic melanin face limitations in terms of sustainability for large-scale production. This lack of a readily available and sustainable melanin source hinders the advancement of research on its potential applications.

This doctoral thesis explores the application potential of fungal melanin as a novel biopolymer for environmental applications. Building upon prior research on the synthesis and characterization of fungal melanin extracted from Exophiala pisciphila (Zhan et al., 2011) or Spissiomyces endophytica (Suwannarach et al., 2019), this work focuses on utilizing DHN-melanin as a source material to explores the potential use in the development of conductive materials that could be utilized in various electronic applications and  the bioremediation of heavy metals from contaminated environments. Different material processing techniques were employed to investigate the properties and functionalities of melanin. Based on the obtained results, the discussion will address several key aspects crucial for the development and design of melanin-based materials for environmental applications. These aspects will encompass the entire process, from melanin synthesis and extraction to processing for the removal of heavy metals and metalloids, and the exploration of potential conductive properties.

To further explore the potential applications of fungal melanin, we employed a two-pronged approach. First, we investigated the metal biosorption capacity of live biomass from two melanized fungi: Exophiala mesophila and Rhinocladiella similis. Second, we analyzed the metallotolerance of various black fungal strains, focusing on the mechanisms behind their tolerance, including both supramolecular interactions and gene expression patterns. This comprehensive approach aimed to elucidate the full biotechnological potential of melanized fungi in metal remediation applications.

Relationship between fungal melanin (DHN), synthesis DOPA -melanin, extraction and structure of melanin

Traditionally, melanin has been isolated from animal sources such as cuttlefish (Sepia spp.) or melanosomes extracted from various animals. However, this dependence on animal sources makes natural melanin production expensive. For example, commercially available melanin from Sepia officinalis can cost upwards of 467 euros per gram from suppliers like Sigma Aldrich. This high cost significantly hinders the development of large-scale applications utilizing melanin.

Recognizing the diverse and valuable functionalities of melanin, research efforts over the past two decades have focused on the extraction and purification of melanin from fungal sources as a more cost-effective alternative. This study contributes to these efforts by employing the fungus Exophiala mesophila for melanin biosynthesis, thereby overcoming the limitations associated with conventional production methods.

This approach offers a cost-effective strategy for natural melanin production, achieving a significant reduction in cost compared to animal-derived sources (approximately 75 euros per gram). However, beyond cost-efficiency, understanding the impact of production and extraction methods on melanin structure is crucial.

Traditional fungal melanin isolation methods often utilize harsh chemical treatments, including prolonged hydrolysis via boiling in mineral acids or bases followed by extensive washing steps with organic solvents (De La Rosa et al., 2017; Pralea et al., 2019). These aggressive procedures can induce significant chemical alterations to the melanin polymer chains (Pralea et al., 2019). Conversely, the primary route for synthetic melanin production involves dopamine oxidation under alkaline conditions using metal catalysts, leading to the formation of polydopamine (PDA) as a common synthetic melanin analog.  While PDA exhibits some properties similar to natural melanin, its structure deviates significantly (Cao et al., 2021. Notably, in this study synthetic DOPA melanin reveals key structural differences, such as a lower abundance of aliphatic chain subunits and a pronounced reduction, or even complete absence, of aromatic/pyrrole stretching vibrations and indole rings using FTIR analysis (Medina-Armijo, et al 2024). In contrast, natural melanins possess over 50% indole and aliphatic subunits (Micillo et al., 2016). This lack of carboxylic acid (–COOH) groups in synthetic melanin leads to substantial variations in its structural features and functionalities compared to natural melanin. In DHN-containing natural melanins, the presence of carboxylic acid (–COOH) groups contributes to several key functionalities. Firstly, they enhance the adsorption surface area for capturing toxic compounds, such as heavy metals.  Secondly, these –COOH groups participate in energy barriers along the carbon-carbon (C-C) backbone, influencing supramolecular interactions like π-π stacking and hydrogen bonding. These interactions play a crucial role in determining the physical and chemical properties of melanin, particularly those relevant to applications like UV radiation protection and semiconductor behavior.

The utilization of black fungi for melanin production offers a compelling alternative that merges the advantages of animal-source extraction and artificial synthesis methods. By providing suitable precursors (e.g., tyrosine, acetyl-CoA, or malonyl-CoA) and optimizing culture conditions, fungi naturally produce melanin within liquid media facilitated by their enzymatic machinery, such as laccase (Meredith and Riesz, 2004). This approach allows for high yields with appropriate fungal strains. For instance, Exophiala mesophila can generate approximately 155 mg of melanin per gram of culture medium. This method demonstrates significant promise for sustainable and scalable industrial melanin production.

Furthermore, fungal melanin retains the inherent properties of natural melanin. The structure of melanin isolated from Exophiala mesophila has been elucidated and compared to existing literature (Eisenman and Casadevall, 2012; Gonçalves et al., 2012; Suwannarach et al., 2019; Elsayis et al., 2022). Employing techniques such as electron paramagnetic resonance (EPR), Fourier-transform infrared (FTIR) spectroscopy, and UV spectroscopy, the authors demonstrated that fungal melanin comprises both DHN subunits and their derivatives (oxidized and radical forms). This structure aligns with the typical allomelanin found in nature and closely resembles melanin extracted from sepia observed in this study.

Following separation from biomass and cellular debris, the melanin solution can be employed as "native melanin" in its liquid form. Alternatively, it can undergo further processing with acid or proteases to yield "purified melanin" in solid form.  However, the chosen extraction method can influence the properties of the final melanin-based products. Acid treatment, while removing trace proteins and lipids, induces the spontaneous assembly of melanin subunits into larger amorphous aggregates also observed in (Cao et al., 2021). Many of the well-documented properties of melanin, such as its remarkable stability and insolubility, arise from this  supramolecular organization (Gonçalves et al., 2012; Suwannarach et al., 2019).  When designing composite materials, it is critical to select the appropriate melanin state (native vs. purified).  Each level of structural organization can expose or conceal specific functional groups, thereby affecting the materials' final properties.

Metal Binding to Melanin extracted vs native black fungi strais

Fungal melanins exhibit remarkable capacity for heavy metal sequestration, as demonstrated by the high absorption of Cr(VI) ions observed in liquid batch experiments.  Natural melanins also sequester reactive metals like Pb(II), Cd(II), Fe(III) and Cu(II), offering protection to biological systems from the detrimental effects of hydroxyl radicals (Liu et al., 2004; Tran-Ly et al., 2020a). This multifaceted metal-binding ability of melanin stems from the presence of diverse functional groups within its structure. These include carboxyl, amine, hydroxyl (phenolic), quinone, and semiquinone groups, which can all serve as potential metal binding sites (Manirethan et al., 2020; Mota et al., 2020; Fahry et al., 2023). Notably, melanin employs a complex binding mechanism, often involving more than one functional group coordinating with the same metal ion.  The specific binding site depends heavily on the nature of the metal itself (Hong and Simon, 2007). For example, the interaction of Pb(II) with fungal melanin was studied, showing high binding affinity at various sites, including catechol (OH), amine (NH), and carboxyl (COOH) groups. In contrast, Cd(II), Zn(II), and Ca(II) bind specifically to carboxyl groups (COOH) (Tran-Ly et al., 2020b; Anh et al., 2022). This phenomenon can lead to competition between functional groups and different metal ions during remediation processes, potentially affecting sorption efficiency. To fully harness the potential of fungal melanin for metal remediation, a deeper understanding of its metal-binding preferences is crucial. This necessitates further remediation studies employing a diverse range of cations. Such investigations will enable a comprehensive assessment of melanin's affinity for different metals and identify those for which fungal melanin can serve as an effective sorbent. In our study we determined that the principal fuctional group in melanin extracted were attribuit to OH- and COOH- as firth binding of metals, however múltiples mechanims were detected such as chemisorption, complexation, electrostatic capacitance, reduction, interaction metal π and cation exchange.

Our studies revealed significant differences in the absorption capacity of live and dead biomass from Exophiala mesophila and Rhinocladiella similis during Cr(VI) and As(V) bioabsorption. Dead biomass with readily available melanin displayed a substantially higher capacity compared to live biomass. This discrepancy arises from the contrasting mechanisms involved: dead biomass offers freely accessible functional groups in the medium, whereas live biomass employs a biological process with intracellular and extracellular transport mechanisms. For instance, E. mesophila demonstrated a marked difference in absorption capacity between live biomass and extracted/purified melanin (qmax: 95.26 vs. 544.84 mg g⁻¹). While both live and dead biomass offer potential for metal removal, they require optimization through different approaches.  (i) Processes reliant on cell growth, while exhibiting slower kinetics, can potentially benefit from extended absorption times to enhance process viability. (ii) Fungal melanin, on the other hand, offers faster absorption kinetics and achieves higher saturation of its metal binding sites. However, this necessitates material replacement in liquid removal systems due to saturation. Furthermore, metal binding to functional groups beyond quinones likely necessitates deprotonation, resulting in pH dependence. This was observed in our Cr(VI) bioabsorption experiments, where 100% metal removal efficiency was achieved at pH 4.

Semiconductivity properties and electron tranfer ions

Chapter 3 (Sections 3.2 and 3.4) focuses on the characterization of fungal melanin's semiconducting potential. This section reports the observation of reversible redox couples attributable to the oxidation and reduction processes involving quinone moieties within the melanin structure.  These interactions are consistent with previous studies on eumelanin (derived from DOPA), where melanin's redox processes are linked to the π-electron conjugation present in its aromatic rings (Orive, 2014; Kumar et al., 2016). Significantly, this thesis work corroborates this interaction by investigating the combined system of fungal melanin and the electrobacterium Geobacter sulfurreducens (GS). The results demonstrate a strong correlation between GS and the quinone redox processes. This interaction leads to a non-reversible electrochemical behavior.  Here, we propose that if quinones are indeed facilitating extracellular electron transfer from GS to the electrode, their reduction (electron gain) would be hindered when GS prioritizes the electrode as the electron acceptor.  In this scenario, the typical reduction peak associated with quinones would be absent in the electrochemical signature, explaining the observed "non-reversible behavior.

To explore the potential application of fungal melanin in electron transfer processes, we established an anaerobic microcosm assay. This assay investigated the ability of fungal melanin to influence the composition of exoelectrogenic bacterial and archaeal communities, specifically focusing on its suppressive effect on methane (CH4) production in rice soil. Similar strategies have been previously reported for materials with properties analogous to melanin, such as biochar and activated carbon (Dong et al., 2021; Lu et al., 2022). The study revealed that fungal melanin exhibits a significant affinity for electrobacteria like Geobacter, Pseudopelobacter, and methanogenic archaea such as Metanosarcina. This strong interaction suggests the occurrence of direct interspecies electron transfer (DIET) within co-cultures of Geobacter species and acetoclastic methanogens (e.g., Methanosaeta and Methanosarcina), as observed in previous studies (Rotaru et al., 2014). The extensive surface area of melanin facilitates electron transfer between microbes and insoluble electron acceptors such as Fe(III) (oxyhydr)oxides. This promotes the reduction of Fe(III) to Fe(II). This process may compete with methanogenesis for available electrons, potentially leading to a decrease in methane (CH₄) emissions. Previous studies suggest a possible inhibition mechanism for methanogenesis (Feng et al., 2012; Sriphirom et al., 2021).

Furthermore, the observed interaction hints at a potential electron-attracting effect exerted by fungal melanin. This effect could potentially alter environmental factors like pH, redox conditions, or nutrient availability, creating an environment less conducive to methanogenesis. Consequently, fungal melanin may modulate DIET between different syntrophic bacteria and methanogens, resulting in a shortened lag phase for CH4 production. This thesis presents the first investigation of fungal melanin for mediating electron transfer through electrobacteria in a strategy for methane reduction within rice field soils. This finding holds significant implications. Natural melanin exhibits a high affinity for Geobacter species, a key electrobacterium.  Furthermore, melanin possesses favorable environmental biocompatibility due to its recalcitrant C=C structures, which contribute to carbon sequestration processes.  Therefore, fungal melanin offers a potential dual benefit: promoting methane reduction and enhancing carbon storage in rice field soils.

Relationship between metallotolerance and mechanims biochemical and expresión gene

Black fungi exhibited remarkable hypertolerance to As(V) and Cr(VI), withstanding concentrations exceeding 12 g L-1 and 2.5 mg L-1, respectively. Four strains stood out for their exceptional tolerance: Exophiala crusticola, Exophiala mesophila, Cyphelophora olivacea, and Rhinocladiella similis. This remarkable adaptability to extreme concentrations was attributed to the conspicuous melanization of these strains. Melanin, in particular, exhibits extraordinary properties against toxic stress, including the ability to generate reactive oxygen species (ROS) and protect hydrolytic enzymes, both of which are crucial for adaptation to toxic substances (Jacobson and Tinnell, 1993). Our research suggests that metallotolerance can exhibit adaptive variations based on the environmental context. Notably, the majority of our strains originated from toxic environments containing arsenic and other metals. This observation was evident in the differences observed between strains of Exophiala mesophila, Aureobasidium pullulans, and Coniosporium uncinatum, with significant variations in radial growth at the hyperconcentrations used in this study. However, further investigation is necessary to determine whether the observed variability in metal tolerance is intrinsic to the species studied or arises from limitations in species identification.

To understand the mechanisms underlying this exceptional tolerance, we employed E. mesophila as a model for an exhaustive analysis of its biochemical changes and gene expression patterns upon exposure to high concentrations of As(V) and Cr(VI). To investigate the relationship between melanin and metal exposure, we initiated a study on the inhibition of melanin DHN, previously characterized in our lab. Previous studies have identified the compound tricyclazole as an inhibitor of melanin DHN via several reductive processes of the acetyl-CoA pathway for its synthesis (Bárcena et al., 2015). SR-FTIRM was also employed to examine the supramolecular response of E. mesophila to tricyclazole.

The effects of tricyclazole exposure on E. mesophila exhibited some similarities to previously reported observations on metal exposure (Liang and Zhou, 2007; Bárcena et al., 2015; Hu et al., 2016; Zhan et al., 2016). Exposure to tricyclazole, a melanin synthesis inhibitor, elicited significant alterations in the protein, DNA, and lipid conformational structures of E. mesophila. These alterations likely influence the organization of complexes responsible for producing secondary metabolites like flaviolin and 2-hydroxy juglone, potentially facilitating the fungus's survival against tricyclazole toxicity and DHN-melanin inhibition (Lee et al., 2003; Bárcena et al., 2015). SR-FTIR analysis revealed changes in aromatic ring vibrations and C=O stretching, characteristic of quinoid structures typically found in melanins, confirming the inhibition of DHN-melanin synthesis.

Analysis of Exophiala mesophila cells exposed to arsenic (native cells) using SR-FTIR spectroscopy suggested a primary impact on proteins at the supramolecular level. This could be attributed to the generation of reactive oxygen species (ROS) upon contact with arsenic ions. Interestingly, the specific protein conformational changes differed between intact cells and those exposed to arsenic. The observed alterations were attributed to modifications in hydrogen bonding within protein amide groups and/or potential metal binding to these groups. Previous studies suggest hydroxyl and amine groups to have high affinity for divalent cations (Fourest et al., 1994; D’Souza et al., 2008). Additionally, arsenic exposure induced changes in the spectral signature of the DNA region, indicative of localized conformational alterations. These alterations could involve pyrimidine dimers, DNA-DNA cross-links, or protein-DNA cross-links. The observed changes in the vibrational modes of the phosphodiester group, particularly their pronounced effect, suggest potential chelating properties. Sugar phosphate esters, the building blocks of DNA, are well-known for their role in metal chelation. This implies that arsenic, a metalloid, might interact with the phosphodiester groups in DNA, potentially altering its synthesis. (Fry et al., 2003) .

Intriguingly, the observed upregulation of genes involved in transport regulation aligns remarkably with the SR-FTIR data, suggesting a potential mechanism for the robust adaptation of E. mesophila to arsenic exposure. These genes likely contribute to maintaining cellular integrity by facilitating controlled influx and efflux of various ions (Na⁺, K⁺, Ca²⁺) across the cell membrane, potentially counteracting the disruptive effects of arsenic on cellular ion homeostasis. Notably, similar observations of hemerythrin cation binding in response to arsenic stress have been reported in Aspergillus oryzae (Liang et al., 2021). Hemerythrin, typically known for iron (Fe²⁺) binding, might be upregulated in E. mesophila to potentially sequester arsenic or other disrupted cations, further protecting cellular components from their detrimental effects. For example, Rhodococcus aetherivorans has also been shown to sequester arsenic within its cells. (Firrincieli et al., 2022). Exophiala mesophila exhibits upregulation of superoxide dismutase (SOD) genes in response to arsenic exposure. This is a well-documented phenomenon in the scientific literature and suggests a cellular defense mechanism against the increased reactive oxygen species (ROS) generated by arsenic stress. SOD enzymes scavenge superoxide radicals, a type of ROS, mitigating their damaging effects on cellular components (Langfelder et al., 2003; Dadachova et al., 2007; Smith and Casadevall, 2019).

Furthermore, the differential gene expression profile points towards another adaptation strategy employed by E. mesophila. The upregulation of genes associated with methyltransferase activity suggests a potential mechanism to facilitate the enhanced uptake of essential nutrients. This might involve modifications to transport proteins or other cellular components mediated by methyltransferases, allowing the fungus to compensate for the disruptions in nutrient acquisition caused by arsenic exposure.

Beyond maintaining cellular integrity and nutrient acquisition, the analysis of metabolic pathways (KEGG system) revealed additional adaptation strategies employed by E. mesophila. These include alterations in pyrimidine metabolism, indicative of prioritized RNA synthesis, likely for the production of new proteins or enzymes necessary for stress response and adaptation. Additionally, upregulated genes associated with oxidative phosphorylation suggest an effort to maintain energy production despite the stress induced by arsenic. Finally, increased proteasome function implies an enhanced protein turnover process, which might be crucial for eliminating misfolded or damaged proteins resulting from arsenic exposure.

Exophiala mesophila exhibits morphological changes in response to arsenic exposure, including colony shape alterations, stronger dark pigmentation, ir-regular in shape and displayed coarser edges under stressful conditions. These changes were initially attributed solely to stress-induced melanin production. However, gene expression analysis in this study did not reveal significantly upregulated expression of melanin synthesis genes. Interestingly, it has been reported that melanin production itself can generate superoxide molecules, potentially indicating the presence of oxidative stress within the fungal cell wall. Despite the potential for melanin to quench and detoxify superoxide ions, suggesting some functional overlap with the antioxidant enzyme superoxide dismutase (SOD), these two mechanisms might act synergistically during arsenic stress. Melanin, situated extracellularly, could potentially buffer the initial oxidative bursts, while intracellular SOD provides further protection. Further research is necessary to fully elucidate the intricate interaction between melanin and reactive oxygen species (ROS) and their combined protective roles.

Furthermore, gene expression analysis suggests that osmotic changes could be the primary drivers of the observed meristematic alterations in arsenic-exposed cells (Figure X). These osmotic changes might involve dehydration and depletion of essential ions (Na+, K+, Ca2+). While oxidative stress undoubtedly plays a role, dedicated studies on osmotic stress responses in fungal cells are crucial to definitively validate this hypothesis.

In contrast to tricyclazole exposure, chromium exerts its toxic effects on E. mesophila at the cellular level, causing significant damage to the cell wall, proteins, DNA, polysaccharides, and overall cellular integrity. The potential mechanism of chromium toxicity appears to involve disruption of protein synthesis and metal binding within the cell. One of the fungus's defense strategies against chromium toxicity involves the increased generation of reactive oxygen species (ROS). However, the subsequent oxidative stress triggered by Cr(VI) exposure can ultimately lead to apoptosis or autophagy through mechanisms like mitochondrial damage, cytochrome c release, DNA fragmentation, phosphatidylserine exposure, and metacaspase activation.

Exposure to chromium triggers rapid changes in gene expression, contrasting with the significant supramolecular differences observed through SR-FTIR analysis. Notably, genes associated with cellular detoxification are upregulated, including those encoding mercury reductase, NADPH dehydrogenase quinone, and peroxisomal catalase. This suggests the activation of defense mechanisms against chromium-induced stress. Furthermore, chromium exposure disrupts various amino acid metabolic pathways, particularly those linked to glutathione, a cellular antioxidant crucial for detoxification, osmoprotection, and energy metabolism. Additionally, chromium disrupts protein synthesis, actin cytoskeleton regulation, and autophagy. Pathways like glycolysis, the pentose phosphate pathway, oxidative phosphorylation, and fatty acid degradation, all essential for energy production, might also be disrupted by chromium exposure. Finally, chromium exposure impacts purine and pyrimidine metabolism, which provides building blocks for DNA and RNA synthesis. These combined effects highlight the widespread cellular disruption caused by chromium exposure.

Intriguingly, chromium exposure appears to induce the metabolic activity of tyrosine, tryptophan, and phenylalanine, ultimately leading to melanin production via the dopa-melanin pathway. This finding contrasts with the previously observed tricyclazole-induced inhibition of DHN-melanin synthesis in E. mesophila, as supported by the relevant literature on this fungal strain.  This observation suggests that E. mesophila possesses the remarkable ability to produce melanin through distinct pathways depending on the specific environmental stress encountered.

However, it is essential to acknowledge that increased tyrosine metabolism cannot be definitively linked solely to melanin synthesis. It could also contribute to protein synthesis for fungal growth, or alternatively, tyrosine degradation could serve as an energy source during nutrient scarcity. Interestingly, previous studies have reported the overexpression of tyrosine metabolism in Exophiala pisciphila; however, a connection to dopa-melanin production was not established in that instance (Zhao et al., 2015).

Anh, N., Ly, T., Fink, S., and Linder, M. (2022). FUNGAL MELANIN AND ITS COMPOSITES FOR WATER REMEDIATION AND WOOD TREATMENT.

Bárcena, A., Petroselli, G., Velasquez, S. M., Estévez, J. M., Erra-Balsells, R., Balatti, P. A., et al. (2015). Response of the fungus Pseudocercospora griseola f. mesoamericana to Tricyclazole. Mycol. Prog. 14. doi: 10.1007/s11557-015-1102-7.

Cao, W., Zhou, X., McCallum, N. C., Hu, Z., Ni, Q. Z., Kapoor, U., et al. (2021). Unraveling the structure and function of melanin through synthesis. J. Am. Chem. Soc. 143, 2622–2637. doi: 10.1021/JACS.0C12322/ASSET/IMAGES/MEDIUM/JA0C12322_0012.GIF.

D’Souza, L., Devi, P., Divya Shridhar, M. P., and Naik, C. G. (2008). Use of Fourier Transform Infrared (FTIR) Spectroscopy to Study Cadmium-Induced Changes in Padina Tetrastromatica (Hauck). Anal. Chem. Insights 3, 135. doi: 10.4137/117739010800300001.

Dadachova, E., Bryan, R. A., Huang, X., Moadel, T., Schweitzer, A. D., Aisen, P., et al. (2007). Ionizing Radiation Changes the Electronic Properties of Melanin and Enhances the Growth of Melanized Fungi. PLoS One 2, e457. doi: 10.1371/JOURNAL.PONE.0000457.

De La Rosa, J. M., Martin-Sanchez, P. M., Sanchez-Cortes, S., Hermosin, B., Knicker, H., and Saiz-Jimenez, C. (2017). Structure of melanins from the fungi Ochroconis lascauxensis and Ochroconis anomala contaminating rock art in the Lascaux Cave. Sci. Reports 2017 71 7, 1–11. doi: 10.1038/s41598-017-13862-7.

Dong, D., Li, J., Ying, S., Wu, J., Han, X., Teng, Y., et al. (2021). Mitigation of methane emission in a rice paddy field amended with biochar-based slow-release fertilizer. Sci. Total Environ. 792, 148460. doi: 10.1016/j.scitotenv.2021.148460.

Eisenman, H. C., and Casadevall, A. (2012). Synthesis and assembly of fungal melanin. Appl. Microbiol. Biotechnol. 93, 931–940. doi: 10.1007/S00253-011-3777-2/FIGURES/2.

Elsayis, A., Hassan, S. W. M., Ghanem, K. M., and Khairy, H. (2022). Optimization of melanin pigment production from the halotolerant black yeast Hortaea werneckii AS1 isolated from solar salter in Alexandria. BMC Microbiol. 22, 1–16. doi: 10.1186/s12866-022-02505-1.

Fahry, Kh., Ghoniem, A. A., Al-Otibi, F. O., Helmy, Y. A., El Hersh, M. S., Elattar, K. M., et al. (2023). A Comparative Study of Cr(VI) Sorption by Aureobasidium pullulans AKW Biomass and Its Extracellular Melanin: Complementary Modeling with Equilibrium Isotherms, Kinetic Studies, and Decision Tree Modeling. Polymers (Basel). 15. doi: 10.3390/polym15183754.

Feng, Y., Xu, Y., Yu, Y., Xie, Z., and Lin, X. (2012). Mechanisms of biochar decreasing methane emission from Chinese paddy soils. Soil Biol. Biochem. 46, 80–88. doi: 10.1016/J.SOILBIO.2011.11.016.

Firrincieli, A., Zannoni, D., Donini, E., Dostálová, H., Rädisch, R., Iommarini, L., et al. (2022). Transcriptomic Analysis of the Dual Response of Rhodococcus aetherivorans BCP1 to Inorganic Arsenic Oxyanions. Appl. Environ. Microbiol. 88. doi: 10.1128/AEM.02209-21/SUPPL_FILE/AEM.02209-21-S0002.XLSX.

Fourest, E., Canal, C., and Roux, J. C. (1994). Improvement of heavy metal biosorption by mycelial dead biomasses (Rhizopus arrhizus, Mucor miehei and Penicillium chrysogenum): pH control and cationic activation. FEMS Microbiol. Rev. 14, 325–332. doi: 10.1111/J.1574-6976.1994.TB00106.X.

Fry, F. H., Jensen, P., Kepert, C. M., and Spiccia, L. (2003). Macrocyclic copper(II) and zinc(II) complexes incorporating phosphate esters. Inorg. Chem. 42, 5637–5644. doi: 10.1021/IC026091D/SUPPL_FILE/IC026091DSI20030612_085525.CIF.

Gonçalves, R. C. R., Lisboa, H. C. F., and Pombeiro-Sponchiado, S. R. (2012). Characterization of melanin pigment produced by Aspergillus nidulans. World J. Microbiol. Biotechnol. 28, 1467–1474. doi: 10.1007/s11274-011-0948-3.

Hong, L., and Simon, J. D. (2007). Current understanding of the binding sites, capacity, affinity, and biological significance of metals in melanin. J. Phys. Chem. B 111, 7938–7947. doi: 10.1021/JP071439H/ASSET/IMAGES/LARGE/JP071439HF00009.JPEG.

Hu, X. J., Liu, Z. X., Wang, Y. Di, Li, X. N., Hu, J., and Lü, J. H. (2016). Synchrotron FTIR spectroscopy reveals molecular changes in Escherichia coli upon Cu2+ exposure. Nucl. Sci. Tech. 27, 1–8. doi: 10.1007/s41365-016-0067-9.

Jacobson, E. S., and Tinnell, S. B. (1993). Antioxidant function of fungal melanin. J. Bacteriol. 175, 7102–7104. doi: 10.1128/jb.175.21.7102-7104.1993.

Kumar, P., Di Mauro, E., Zhang, S., Pezzella, A., Soavi, F., Santato, C., et al. (2016). Melanin-based flexible supercapacitors. J. Mater. Chem. C 4, 9516–9525. doi: 10.1039/C6TC03739A.

Langfelder, K., Streibel, M., Jahn, B., Haase, G., and Brakhage, A. A. (2003). Biosynthesis of fungal melanins and their importance for human pathogenic fungi. Fungal Genet. Biol. 38, 143–158. doi: 10.1016/S1087-1845(02)00526-1.

Lee, J. K., Jung, H. M., and Kim, S. Y. (2003). 1,8-Dihydroxynaphthalene (DHN)-melanin biosynthesis inhibitors increase erythritol production in Torula corallina, and DHN-melanin inhibits erythrose reductase. Appl. Environ. Microbiol. 69, 3427–3434. doi: 10.1128/AEM.69.6.3427-3434.2003.

Liang, J., Liu, J., Cheng, T. Q., and Song, W. (2021). Comparative Transcriptome Analysis Providing Resistance Mechanism of Aspergillus oryzae Under Arsenate Stress. Geomicrobiol. J. 38, 426–435. doi: 10.1080/01490451.2021.1877854.

Liang, Q., and Zhou, B. (2007). Copper and manganese induce yeast apoptosis via different pathways. Mol. Biol. Cell 18, 4741–4749. doi: 10.1091/mbc.E07-05-0431.

Liu, Y., Hong, L., Kempf, V. R., Wakamatsu, K., Ito, S., and Simon, J. D. (2004). Ion-exchange and adsorption of Fe(III) by Sepia melanin. Pigment Cell Res. 17, 262–269. doi: 10.1111/j.1600-0749.2004.00140.x.

Lu, Y., Liu, Q., Fu, L., Hu, Y., Zhong, L., Zhang, S., et al. (2022). The effect of modified biochar on methane emission and succession of methanogenic archaeal community in paddy soil. doi: 10.1016/j.chemosphere.2022.135288.

Manirethan, V., Raval, K., and Balakrishnan, R. M. (2020). Adsorptive removal of trivalent and pentavalent arsenic from aqueous solutions using iron and copper impregnated melanin extracted from the marine bacterium Pseudomonas stutzeri. Environ. Pollut. 257, 113576. doi: 10.1016/J.ENVPOL.2019.113576.

Meredith, P., and Riesz, J. (2004).  Radiative Relaxation Quantum Yields for Synthetic Eumelanin ¶ . Photochem. Photobiol. 79, 211–216. doi: 10.1111/J.1751-1097.2004.TB00012.X.

Micillo, R., Panzella, L., Koike, K., Monfrecola, G., Napolitano, A., and D’Ischia, M. (2016). “Fifty Shades” of Black and Red or How Carboxyl Groups Fine Tune Eumelanin and Pheomelanin Properties. Int. J. Mol. Sci. 2016, Vol. 17, Page 746 17, 746. doi: 10.3390/IJMS17050746.

Mota, E. A., Felestrino, É. B., Leão, V. A., and Guerra-Sá, R. (2020). Manganese (II) removal from aqueous solutions by Cladosporium halotolerans and Hypocrea jecorina. Biotechnol. Reports 25, e00431. doi: 10.1016/J.BTRE.2020.E00431.

Orive, A. G. (2014). Electrogeneración de películas ultradelgadas de melanina: nanoestructura, electrocatálisis, conductividad, magnetismo y fotorrespuesta.

Pralea, I. E., Moldovan, R. C., Petrache, A. M., Ilieș, M., Hegheș, S. C., Ielciu, I., et al. (2019). From Extraction to Advanced Analytical Methods: The Challenges of Melanin Analysis. Int. J. Mol. Sci. 20. doi: 10.3390/IJMS20163943.

Rotaru, A. E., Shrestha, P. M., Liu, F., Markovaite, B., Chen, S., Nevin, K. P., et al. (2014). Direct interspecies electron transfer between Geobacter metallireducens and Methanosarcina barkeri. Appl. Environ. Microbiol. 80, 4599–4605. doi: 10.1128/AEM.00895-14/ASSET/DE9D6F24-9C8B-4D33-ADC0-76C2364EC6FC/ASSETS/GRAPHIC/ZAM9991055120004.JPEG.

Smith, D. F. Q., and Casadevall, A. (2019). The role of melanin in fungal pathogenesis for animal hosts. Curr. Top. Microbiol. Immunol. 422, 1–30. doi: 10.1007/82_2019_173.

Sriphirom, P., Chidthaisong, A., Yagi, K., Tripetchkul, S., Boonapatcharoen, N., and Towprayoon, S. (2021). Effects of biochar on methane emission, grain yield, and soil in rice cultivation in Thailand. Carbon Manag. 12, 109–121. doi: 10.1080/17583004.2021.1885257.

Suwannarach, N., Kumla, J., Watanabe, B., Matsui, K., and Lumyong, S. (2019). Characterization of melanin and optimal conditions for pigment production by an endophytic fungus, Spissiomyces endophytica SDBR-CMU319. PLoS One 14, 1–15. doi: 10.1371/journal.pone.0222187.

Tran-Ly, A. N., Ribera, J., Schwarze, F. W. M. R., Brunelli, M., and Fortunato, G. (2020a). Fungal melanin-based electrospun membranes for heavy metal detoxification of water. Sustain. Mater. Technol. 23, e00146. doi: 10.1016/j.susmat.2019.e00146.

Tran-Ly, A. N., Ribera, J., Schwarze, F. W. M. R., Brunelli, M., and Fortunato, G. (2020b). Fungal melanin-based electrospun membranes for heavy metal detoxification of water. Sustain. Mater. Technol. 23, e00146. doi: 10.1016/J.SUSMAT.2019.E00146.

Zhan, F., He, Y., Yang, Y., Li, Y., Li, T., and Zhao, Z. (2016). Effects of Tricyclazole on Cadmium Tolerance and Accumulation Characteristics of a Dark Septate Endophyte (DSE), Exophiala pisciphila. Bull. Environ. Contam. Toxicol. 96, 235–241. doi: 10.1007/s00128-015-1676-4.

Zhan, F., He, Y., Zu, Y., Li, T., and Zhao, Z. (2011). Characterization of melanin isolated from a dark septate endophyte (DSE), Exophiala pisciphila. World J. Microbiol. Biotechnol. 27, 2483–2489. doi: 10.1007/s11274-011-0712-8.

Zhao, D., Li, T., shen, M., Wang, J., and Zhao, Z. (2015). Diverse strategies conferring extreme cadmium (Cd) tolerance in the dark septate endophyte (DSE), Exophiala pisciphila: Evidence from RNA-seq data. Microbiol. Res. 170, 27–35. doi: 10.1016/J.MICRES.2014.09.005.